## Slide 1: Semiconductor Polaritons (Inherently Infrared)

## Slide 2: Many types of Polaritons in 2D Materials
eB < 0
eA > 0
–
–
–
+
+
+
–
+
+
–
–
–
+
+
Plasmon-polaritons
(graphene, black P )
Phonon-polaritons,
(hBN, topological
insulators, TMDs)
Exciton-polaritons
(MoS2, WSe2)
Cooper-pair
polaritons
(Cuprates, FeSe)
Magnon-polaritons,
(Cr2Ge2Te6 )
–
–
–
–
lP
l0
incident wavelength
polariton wavelength
D. N. Basov, M. M. Fogler, and F. J. García de Abajo Science 354, 195 (2016).
Slide courtesy of D. Basov
Another review: Low, Chaves, Caldwell, et al. Nature Materials, 16 182 (2017).

## Slide 3: Type 1: SPPs

## Slide 4: Type 1: Surface Plasmon Polaritons
Carrier densities in metals are too high for IR/THz
Doped Semiconductors  IR/THz SPPs
Operating frequency dictated by material and carrier density
Losses dictated by material and mobility
A. Boltasseva and H. Atwater, Science, vol. 331, pp. 290-291, (2011).
mobility
carrier density

## Slide 5: Dispersion Relationship
Volume
plasmon
What does the dispersion actually mean?
  Higher k  smaller wavelength/higher confinement
  Bigger mismatch with momentum of light
Polaritonic material
Dispersion dictates compression of wavelength and therefore focusing of EM fields
+
-
-
charge
+
+

## Slide 6: Momentum Mismatch
Volume
plasmon
To achieve high confinement  need high k-modes
Large momentum mismatch
Photon speedbumps
Recent Review:
J.D. Caldwell, et al., Nanophotonics, 4(1), 44-68 (2015).
charge
Photon
No Polariton
Polariton!
charge
Photon

## Slide 7: Speedbumps for Light!
High Index Prism
Kretschmann
Otto
d
i
kSPP
ki
Grating
Nanostructures

## Slide 8: Plasmons in TCOs
H.w. Lee, et al. Nano Lett., 2014, 14 (11), pp 6463–6468
PlasMOStor
N. Kinsey, Optica, vol. 2, no. 7, 2015.
Fast Carrier Dynamics
J. Kim et al., Optica 3(3), 339-346 (2016).
TCO SPPs
M.A. Noginov, et al., APL 99, 021101 (2011).
Ag
Au
ITO
AZO
ZITO
ENZ Effects

## Slide 9: Carrier Control of Emissivity
ZnO-based modulation
  Long carrier lifetime, low req. fluence
UV LED illumination (10mW/cm2)
Opens the door to large area modulation
  Spatially tailor emissivity / apparent temperature
Metamaterial Schematic
Experimental Emissivity Modulation
Coppens, et al. Adv. Mat. In press (2017).

## Slide 10: Plasmonics with Doped Semiconductors
D.C. Adams, et al. Appl. Phys. Lett., 96, 201112 (2010).
GaAs-SPP Beam Steering
Localized SPPs in InAs
S. Law, et al., Nano-Letters, 2013.
S. Law, et al. JVSTB 31, 03C121 (2012).
Carrier Density
3x1018cm-3
9x1019cm-3
InAs – wp doping dep.
Ge-doped GaN
Kirste, R. et al. Appl. Phys. Lett. 103, 242107 (2013).
Doped Si Nanowires
L-W. Chou et al, Angew. Chem. Int. Ed. 52 8079 (2013)

## Slide 11: Doped CdO as a Low-Loss SPP Material
Material | [cm-3] | Mobility [cm2/V·s ] | ε1=0 [cm-1] | ε2 at ε1=0 | ε2 at ε1=-2
CdO:Dy | 9.94x1019 | 474 | 2770 | 0.19 | 0.30
CdO:Dy | 3.70x1020 | 359 | 5350 | 0.13 | 0.20
AZO (2 wt%)* | 7.2x1020 | 47.6 | 6970 | 0.21 | 0.39
ITO (10 wt%)* | 7.7x1020 | 36 | 7122 | 0.69 | 1.29
GaAs** | 1x1019 | 1000 | 1005 | 1.26 | 1.63
InAs+ | 7.5x1019 | 360 | 1785 | 2.00 | 2.60
**Szmyd, D. M., Hanna, M. C. & Majerfeld, A. Heavily doped GaAs:Se. II. Electron mobility. J. Appl. Phys. 68, 2376–2381 (1990)
+ Law, S., Adams, D. C., Taylor, A. M. & Wasserman, D. Mid-infrared designer metals. Opt. Express 20, 12155–12165 (2012).
* Naik, G. V., Shalaev, V. M. & Boltasseva, A. Alternative plasmonic materials: Beyond gold and silver. Adv. Mater. 25, 3264–3294 (2013).
4000
3000
2000
40
50
60
40
50
60
Wavenumber (cm-1)
Angle (degrees)
t=510 nm N=1.5x1020 cm-3 m=452 cm2/Vs
t=280 nm N=3.3x1020 cm-3 m=435 cm2/Vs

## Slide 12: Broad Spectral Coverage for IR SPPs
1017
1019
1021
1023
carrier density [cm-3]
100
101
102
103
104
mobility [cm2/V·s]
Dy:CdO
8 -12 µm
3-5 µm
High Q plasmons in both MW and LWIR atmospheric windows

## Slide 13
–
–
–
+
+
+
–
+
+
–
–
–
+
+
Plasmon-polaritons
(graphene, black P )
–
–
–
–
Volume
plasmon
wIR
1/lSPP
eB < 0
eA > 0
Slide courtesy of D. Basov
lP
l0
incident wavelength
polariton wavelength
Probing SPPs in 2D Materials:
SNOM

## Slide 14: Probing SPPs in 2D Materials: SNOM of Graphene
lp/2
Chen et al. Nature 487, 77 (2012)
Zhe Fei et al. Nature 487 82 (2012)
–
–
–
+
+
+
–
+
+
–
–
–
+
+
Plasmon-polaritons
–
–
–
–
eB < 0
eA > 0
l0/lP=80-200
Slide courtesy of D. Basov
Volume
plasmon
wIR
1/lSPP
lP
l0
incident wavelength
polariton wavelength
IR

## Slide 15: Graphene SPPs: Gate Tuning
SPP wavelength is changed w/ incident frequency
But it can also be tuned by changing carrier density!
  Not realistic in metals or many highly doped semiconductors
Graphene SPPs are ideal for tuning THz to MWIR (up to 0.01 e/atom)
–
–
–
Volume
plasmon
1/lSPP
Zhe Fei et al. Nature 487 82 (2012)
Chen et al. Nature 487, 77 (2012).

## Slide 16: SPPs in 2D Materials: Beyond Graphene
State of the art in graphene SPPs
  Published: 500 fs lifetimes in hBN encapsulated graphene (Woessner, et al. Nat. Mat. (2015).  25 cycles before decay to 1/e; confinement to 150x <l (free-space)
  Basov recent talk  ballistic SPP propagation at cryogenic temperatures (SNOM)
A wide range of other 2D materials can support SPPs
  Ready to be explored!
Low, Chaves, Caldwell, et al. Nature Materials, 16 182 (2017).