## Slide 1: Semiconductor Nanophotonics
Josh Caldwell
Vanderbilt University June 2017
josh.caldwell@Vanderbilt.edu
Ettore Majorana Summer School, Erice, Italy; July 29, 2017

## Slide 2: Outline
Semiconductor Basics
  Bandstructure/defects
  Phonons
Dielectric Functions
  Electronic & vibrational contributions
  ENZ and high index modes
Surface Plasmon Polaritons
  Bulk semiconductor plasmons
  2D material plasmons
Surface Phonon Polaritons
  Initial work
  Carrier-induced tuning
  What makes a ‘good’ SPhP material?
Hyperbolic Semicondutors
  Hyperbolicity in hBN
  Nature and Metamaterial Hyperbolicity
Atomic Scale Heterostructures
  Electromagnetic hybrids
  Crystalline hybrids

## Slide 3: Energy Bands in Crystals
Hybridization of atomic orbitals due to bonding
  In diatomic species  bonding/anti-bonding orbitals
  In large atom limit  bands form due to many overlapping states
Highest filled band referred to as valence band (HOMO in chemistry-speak)
Lowest unfilled band referred to as conduction band (LUMO)
Loosely speaking size of band gap defines material operation
  Insulator  Big band gap
  Conductor  Band overlap
  Semiconductor  just right… err… somewhere in between
http://micro.magnet.fsu.edu/primer/java/lasers/diodelasers/index.html

## Slide 4: Types of semiconductors
Zinc Oxide nanowires
Cadmium Oxide
Old Soviet Cu2O Diodes
Oxides
B. Radisavljevic, A. Radenovic, J. Brivio, V. Giacometti, A. Kis
Nat. Nanotechnol., 6 (2011), pp. 147-150
Layered
Molybdenum Disulfide
Bao, Material Matters 2007, 2.3, 4.
Organic
Ternaries/Quarternaries
Mercury Cadmium Telluride (MCT)
Indium Gallium Nitride (InxGa1-xN)
Teledyne
Wikipedia
CVD Equipment Corp.
Binary
Silicon carbide
Gallium Nitride
Aluminum nitride
Gallium Phosphide
Hexatech
Wikipedia
Semiwafer
Elemental
silicon
Gray tin: semiconductor!
white tin: metal
Periodictable.ru

## Slide 5: Semiconductor growth
Goal: High quality single crystal material boules
Number of methods
  Czochralski, Acheson…
Perhaps most famous is Czochralski
  Single crystal silicon boules for wafer cuts
Bulk growth
Czochralski method
Epitaxial Growth
Goal: High quality layers
Molecular Beam Epitaxy (MBE)
  – single layer precision
  – Physical process
Chemical Vapor Deposition (CVD)
  – few nm precision
  – chemical process
  Vapor-phase epitaxy (VPE); also liquid- and solid-
  Metal-organic CVD
Atomic-Layer Epitaxy (ALE)
MBE
http://iramis.cea.fr/en/Phocea/Vie_des_labos/Ast/ast_sstechnique.php?id_ast=494
CVD
https://www.withfriendship.com/user/svaruna/Chemical-vapor-deposition.php
Layer/Nano Deposition
Goal: layers/coatings
Pulsed Laser Deposition (PLD)
Sputtering/Evaporation
Atomic Layer Deposition (ALD)
  Conformal, atomic scale control of thin films
PLD
http://www.rmvac.com/products/vacuum-equipments/pld.html
Atomic Layer Deposition
Beneq

## Slide 6: Electronic Band Structure
Band Structure & Brillouin Zone for Si
Ok, so I simplified things
Direct bandgap
Indirect bandgap
  Nature Photonics 7, 264–265 (2013)
Scientific Reports 5, 17902 (2015).
Effective Mass
Near VB/CB edge:
High symmetry in crystals allows for simplified band structure

## Slide 7: Defects in Semiconductors
Defects cause localized disturbances in the lattice periodicity and thus band structure is preserved
  Induce isolated states within band structure
  Can induce states within the band gap
Many types, but two primary categories
  Point defects
  Extended defects
Impact of defects
  Reduce carrier lifetime
  Induce or eliminate luminescence
  Can act as current traps
http://mechanicstips.blogspot.com/2012/10/materials-crystal-defect.html
“Luminescence - An Outlook on the Phenomena and their Applications”,
Edited by J. Thirumalai, Ch. 10, Fig. 1, Publisher: InTech, DOI: 10.5772/62517

## Slide 8: The Beauty of Defects
The Hope Diamond The biggest Blue Diamond
Yellow Diamonds
http://www.igr-global.com/blog-detail/the-science-of-precious-pink-diamonds-plastic-deformation
Nitrogen Defects
Boron Defects
Pink/Red Diamonds

## Slide 9: Defect-based Single Photon Emitters
0
0.2
0.4
0.6
0.8
1
1.2
-40
-20
0
20
40
t (ns)
g(2)(t)
637nm
NV Center in Diamond
Ensemble PL of VSi in 4H-SiC at 20 K
Fuchs, F. et al., Nat. Comm 6:7578 doi: 10.1038/ncomms8578 (2015).
Courtesy of S. Carter, NRL
Si Vacancies in SiC
Courtesy of S. Carter, NRL
Room-temp single photon emission in hBN
T.T. Tran, et al. Nat. Nano11, 37-41 (2016).
Room-temp single photon emission in GaN
A.M. Bethane, et al. Adv. Mat. 29(12) (2017)

## Slide 10: Dopants: The Best Defects
Certain impurities and corresponding defects states are beneficial
  Impurities w/ extra electron in outer shell  n-type defect (electron donor)
  Impurities w/ less electrons in outer shell  p-type defect (electron acceptor)
Shallow energy states (donor/acceptor levels) provide additional free carriers
Increases conductivity by moving Fermi level (chem. Pot.) within bandgap
http://hyperphysics.phy-astr.gsu.edu/hbase/Solids/dope.html#c3
http://nptel.ac.in/courses/115102025/module2/2.html
EF/EC (EV) crossover:
Metal/semiconductor transition
‘degenerate doping’

## Slide 11: Revisiting the Definition of Semiconductors
Is Diamond a Semiconductor?
1. yes, 2. no, 3. it depends
C.B.
V.B.
@kT=0
@kT>0
@kT>0
Intrinsic
Extrinsic
Intrinsic
Eg
C.B.
V.B.
@kT=0
Eg
@kT>0
Insulator?
@kT>0
Semiconductor
@kT>0
@kT>0
Semi-insulating
Semiconductor
Semiconductor
Semi-insulating
Narrow gap
Wide gap

## Slide 12: Revisiting the Definition of Semiconductors
Is Diamond a Semiconductor?
3. It depends…

## Slide 13: Optical effects of confinement
In bulk crystals form bands
Shift back towards nanoscale  approaches individual states (particle in a box)
  Causes lowest energy transitions to increase (quantum confinement)
  Confinement onset occurs when structure size  exciton (e-h pair) wavefunction size
Al Balushi, et al. Nat. Mat. 15, 1166 (2016).
2D GaN
OD: CdSe QDs
3D: Bulk
2D: quantum well
1D: quantum wire
0D: quantum dot
Koole, et al. Ch. 2 in “Nanoparticles”, Springer-Verlag, Berlin (2014). DOI: 10.1007/978-3-662-44823-6

## Slide 14: Controlling MoS2 bandstructure with thickness
MoS2 reduced layer thickness  increase in photoluminescence!
As thickness is reduced
  Direct gap at K-point is nominally unchanged
  Indirect gap is increased
  For monolayers
K-pt  electrons localized to d-orb. (Mo)
  Weak interlayer coupling!
G-pt/indirect gap  linear Comb. of d-orb. (Mo) w/ anti-bonding pz-orb. (S)
  Strong interlayer coupling!
Bulk
4-layers
2-layers
monolayer
A. Splendiani, et al. Nano Lett. 10(4), 1271-1275 (2010).
http://nanotribology.mse.ufl.edu/research.html

## Slide 15: Phonons
Each molecule has a set of fundamental vibrations
In a linear chain standing waves are established
  Long-wavelength acoustic
  Short wavelength optic
In a crystal set of normal modes are established
  Results in phonon dispersion
  Brillouin zones can be used to understand electron-phonon interactions
https://commons.wikimedia.org/wiki/File%3A1D_normal_modes.gif
http://www1.lsbu.ac.uk/water/water_vibrational_spectrum.html
Molecular Vibrations
Vibrations in a 1D chain
http://exciting-code.org/boron-animate-phonons
Vibrations in a 3D Crystal: Phonons
https://en.wikipedia.org/wiki/Phonon
https://en.wikipedia.org/wiki/ Phonon
https://www2.warwick.ac.uk/fac/sci/physics/current/postgraduate/regs/mpags/ex5/phonons/

## Slide 16: Optic Phonons
Si
c-SiC
Two types of optic phonon
  Transverse Optic (TO)
  Longitudinal Optic (LO)
Both types are degenerate
Two types of optic phonon
Transverse ED
Longitudinal ED
X
J.D. Caldwell, et al., Nanophotonics, 4(1), 44-68 (2015).
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
Si
C
C
C
Si
Si
Si
C
C
C
Si
Si
Si
Si
Si
C
C
Si
Si
C
C
Does this picture change for SiC?
No
Yes, TO shifts to higher energy
Yes, LO shifts to higher energy
Zzzz….

## Slide 17: Optic Phonons
Si
c-SiC
Does this help?
No
Yes, TO shifts to higher energy
Yes, LO shifts to higher energy
Zzzz….
Two types of optic phonon
Transverse ED
Longitudinal ED
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
J.D. Caldwell, et al., Nanophotonics, 4(1), 44-68 (2015).
X

## Slide 18: Polar Optic Phonon Splitting
Si
c-SiC
Polar crystals – optic phonons no longer degenerate
  LO phonon like a parallel plate capacitor: separating charges induces restoring force
  LO phonon shifts to higher energies
  Induces LO-TO phonon splitting  the “Reststrahlen band”
Transverse Optic (TO)
    If polar, can couple to an external electric field (e.g. infrared light)
Longitudinal Optic (LO)
    If polar, can couple to internal electric field from free carriers
Two types of optic phonon
Transverse ED
Longitudinal ED
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
J.D. Caldwell, et al., Nanophotonics, 4(1), 44-68 (2015).
{
LO-TO splitting Reststrahlen
Does this help?
No
Yes, TO shifts to higher energy
Yes, LO shifts to higher energy
Zzzz….

## Slide 19: LOPC Effect
In polar semiconductors, high free carrier conc. creates macroscopic E fields
LO phonons and bulk plasma can couple due to E field results
This coupling causes the LO mode to shift from wLO  w+LPP
  LOPC (LO phonon-plasmon coupled mode)
Raman – shift and broadening
IR – ‘softening’
Caldwell, et al. JAP 101, 093506 (2007).
Spann et al. PHYSICAL REVIEW B 93, 085205 (2016)
D. Talwar, et al., Semicond. Sci. Tech. 27, 115019 (2012).

## Slide 20: Electronic Transitions in Semiconductors
Many types of electronic transitions
Result in changes in reflection, absorption and transmission
Can be observed as luminescence or lack thereof
Modify carrier recombination pathways
  Modify lifetime and carrier mobilities
Conduction band
Valence band
Direct Gap Transition
Conduction band
Valence band
Indirect Gap Transition
Conduction band
Valence band
Donor/Acceptor Transitions
Conduction band
Valence band
Defect States
Defect-Mediated Transitions
Conduction band
Valence band
Intraband Transitions
Conduction band
Interband Transitions
Higher Energy Conduction band

## Slide 21: Dielectric Function: Electronic Transitions
Lots of physical processes effect dielectric function
Properties impacting electronic and optical regimes are different
Optical regime (electronic and atomic/vibrational)
Electronic Transitions
  Band gap
  Carrier based
  Interband

## Slide 22: Influence of Free Carriers: Drude Term
Plasma frequency (wp)  fastest electrons (holes) oscillation frequency
At w<wp electrons coherently oscillate
Creates a surface field that opposes the incident light (EM field); high reflectivity
  Negative real part of permittivity
e’(l) < 0
wp
Ag
electrons
mobility
carrier density

## Slide 23: Influence of Polar Optic Phonons: TOLO Term
e’(l) <0
Phonon Polariton Resonances
At wLO>w>wTO, polar lattice vibrations collectively oscillate at incident l through optical phonon excitations
Creates a surface field that opposes the incident light (EM field); high reflectivity
  Negative real part of permittivity
SiC Epilayer
d-
d+
Recent Review:
J.D. Caldwell, et al., Nanophotonics, 4(1), 44-68 (2015).

## Slide 24: Influence of Free Carriers on Polar Optic Phonons
Lyddane-Sachs-Teller Relationship
TOLO contribution
Drude contribution
LOPC effect!

## Slide 25: ENZ condition w/in dielectric functions
Where to find ENZ?
N. Engheta, Science, Vol. 340 no. 6130 pp. 286-287, 2013
Supercoupling Effect
PHYSICAL REVIEW B 75, 155410 2007
Wavefront Engineering
Air Hole in ENZ
Waveguide from Air
Doped Semiconductors
Polar Dielectrics
Metamaterial Designs
J. Kim, et al. Optica 3(3) 339 (2016).

## Slide 26: Light propagation in high index materials
Ginn, J. C. et al. Phys. Rev. Lett. 108, 097402 (2012).
Kuznetsov, Sci. Rep. 2, 492 (2012).
Staude, I. et al., ACS Nano 7, 7824–7832 (2013).
Yang, Y, et al., Nature Comm. 5, 5753 (2014).
Perfect / Magnetic Reflectors
Valentine et. al. ACS Phot. (2015)
Brener et. al. Optica (2014),
Dielectric “Mie” Resonances
Electric and Magnetic Dipoles
All-dielectric Metamaterials
Nonlinear Enhancement
Kivshar, Neshev et. al. Nano Lett (2014), ACS Phot. (2015)
Phase Manipulation
Brongersma, Science (2014)