VANDERBILT STUDENT VOLUNTEERS FOR SCIENCE

http://studentorgs.vanderbilt.edu/vsvs

Phosphorescence and Fluorescence

2012, Elementary school

GOAL:  To show students the difference between phosphorescence and fluorescence.

I.  Introduction

The differences between incandescence, luminescence, fluorescence and phosphorescence are discussed.

A.  Fluorescence is explained and demonstrated using a blacklight and a secret message written on purple paper.

B.  Phosphorescence is explained and demonstrated using a blacklight and UV detecting

beads.

II. What Materials Fluoresce or Phosphoresce?

Students are given a variety of materials to determine if they phosphoresce or fluoresce.  Students place the material in a small box and irradiate them with a blacklight.  The lid of the box is closed and the materials viewed through a slit in the lid.

III. What kind of light is needed to produce Fluorescence and Phosphorescence?

Students use different LED lights discover what kind of light is needed to make a phosphorescing material glow.

IV. Students make a bracelet with Glow in the Dark beads and braid.

Materials

1 piece of purple paper with a secret message written on it

1 necklace of UV detecting beads (white color)

12 boxes with small slit cut into lid, containing

1 piece of laminated black paper with zinc sulfide on one half and laundry powder on the

other half

1 laminated rectangle of paper with Neon paint on one half and Glow in the Dark paint

on the other half (same color)

12  plastic bags with

4 small rectangles of paper towel

1  Highlighter markers

12 plastic bags with

1 piece of phosphorescent vinyl material

LED lights of different colors (red, white and blue - students will share)

12 black lights

32 1oz cups

1 jar containing about 150  glow in the dark beads (5 per student)

32 strands of glow in the dark braid, with bead knotted at one end

32 Observation sheets

1 box of goggles

I.  Introduction

Tell students that here are two general classifications of visible light.

- Incandescence, is hot light.

Ask students to name some hot objects that give off light.

Some examples are burning wood in fireplaces, incandescent light bulbs, a lit match, and fireworks.

B.  	Luminescence, is cold light, refers to light that a substance emits without an

increase in temperature.

Ask the students to name some objects that give off “cold” light?

Fluorescent light bulbs emit cold light.

This lesson focuses on 2 types of Luminescence – Fluorescence and Phosphorescence.

Explain the difference between Fluorescence and Phosphorescence.

A.  Fluorescence

When the energy source is removed, the fluorescing material stops glowing.

Demonstrating Fluorescence – Secret  Message.

The message has been written on purple paper.  Shine the black light on the paper to make it fluoresce.  Point out that the message does not glow after the black light is turned off.

B.  Phosphorescence

When the energy source is removed, the glowing material continues to emit light for a while.

Demonstrating Phosphorescence in UV Detecting Beads.

Show the students a string of the beads and point out the white color.  Shine a black light on the necklace for about 20 seconds, until the beads change color.  Remove the light - the color slowly fades.

For VSVS information: The change involves a dye molecule absorbing UV energy to produce a different geometric isomer of the molecule.  When the light is removed, the dye molecule rotates back to the more stable form.

Objects which glow in the dark are examples of phosphorescent materials.  They contain a chemical that has the ability to absorb light energy quickly and then emit it slowly.

Distribute goggles for the students to wear while doing this experiment.

II. What Materials Fluoresce or Phosphoresce?

Put the observation chart on the board, and help the students make the correct observations.

Follow the order on the observation sheet.

Note:  The  highlighter pen samples will be prepared by the students (tell them to write their initials on the paper towel).

Show students how to do the following:

1.  Place the first material being investigated inside the box.  Leave the lid off.

2.  Record observations about the color of the material (do this as a class activity) before

it is illuminated.

3.  Turn the black light on and place it upside down over the box so that it is shining into

the box.

4.  Wait about 20 seconds (students can count) and record observations about any

changes in the material (has it changed color, is it glowing,…?) while the blacklight is

on..

5.  Remove the blacklight and close the lid of the box.  Look through the slit to see if the

material is still glowing.  Record the results.

6.  Have the students conclude if the material is fluorescing or phosphorescing.

If the material is still glowing, it is phosphorescing.

If the material stops flowing after the blacklight is removed, the material is fluorescing.

Results

| Material | What Color is it in room light? | How does it change under the blacklight? | Does it glow after the box lid is closed? | Does it Fluoresce or Phosphoresce? |
| --- | --- | --- | --- | --- |
| Laundry Detergent | White | Glows bluish | no | Fluoresce |
| Zinc Sulfide | yellow | Glows yellow | yes | Phosphoresce |
| White paper label | white | Glows with a bluish tinge | no | Fluoresce |
| Neon Paint | Dull color | Glows brightly, same color | no | Fluoresce |
| Glow in the Dark Paint | Dull color | Glows brightly, same color | yes | Phosphoresce |
| Highlighter on paper towel | yellow | Bright yellow | no | Fluoresce |

Background Information

1.  Zinc Sulfide - Phosphoresces.

Materials such as zinc sulfide that phosphoresce are called “phosphors.”  Electrons in zinc sulfide are exited by light energy to higher energy levels.  Then when the light source is removed, the excited electrons gradually return to the lower energy ground state.  During this time the substance appears to glow because the difference in energy between the excited state and the ground state is emitted as light.  Once all the excited electrons have returned to the ground state, the substance ceases to glow.  However, every time the substance is exposed to light the electrons are excited up to a higher energy level so when a phosphorescent substance stops glowing, just turn on the lights for a few minutes to "recharge" the substance.

2.  Laundry Powder – Fluoresces.  Optical brighteners are added to laundry detergent to make clean clothes look whiter.  These additives are called optical brighteners because they absorb UV light and emit visible light through fluorescence.  When optical brighteners are incorporated into textiles, they make the material appear brighter and whiter, thus giving the appearance of being cleaner.

Students see a bluish color immediately after the black light is shone, but the blue color is gone as soon as the black light is removed.  It cannot be seen glowing in the box after the lid is closed.

3.  White paper (fluoresces):  Optical brighteners are added to high quality paper (such as copy paper), but not to cheaper paper towels.

III.  What kind of light is needed to produce Fluorescence and Phosphorescence?

Materials

1 piece of phosphorescent vinyl

Red, blue and white LED lights

Tell the students to gently draw a “squiggle” on the yellow vinyl material, using the LED lights in the following order:

Blue, then White, then Red

Record which LED’s made the material phosphoresce.

Tell students to look at the electromagnetic spectrum on their Instruction sheet.

Long Wavelength 700 nm 					Short wavelength 400 nm		     Lower Energy 1.8 eV				             Higher Energy 3.1 eV

For your Information:  white light contains wavelengths ranging from 400-700nm, with energy in the range 1.8 to 3.1 electron volts.

Tell the students that some materials need UV light to glow, while others (like the zinc sulfide and the vinyl) can be excited with white light.

The energy of the white light needs to be from the higher energy (the blue end) end of the spectrum.  The red light does not have enough energy to make the material phosphoresce.

IV.  Making Glow in the Dark Bracelets.

Pass out the beads and braid and have the students make a bracelet.  Tell the students that this bracelet will glow in the dark after it has been exposed to sunlight.

Lesson ideas were taken from kits from Educational Innovations.

Lesson written by Pat Tellinghuisen, VSVS Program Director, Vanderbilt University

Mel Joesten, Professor Emeritus, Vanderbilt University

Observation Sheet

You must wear goggles while doing this experiment.

Long Wavelength  700 nm					    Short wavelength 400 nm

Lower Energy (about 1.8 eV)			                            Higher Energy (about 3.1eV)

Observation Sheet - Answers

What materials Fluoresce or Phosphoresce?

| Material | What Color is it in room light? | How does it change under the blacklight? | Does it glow after the box lid is closed? | Does it Fluoresce or Phosphoresce? |
| --- | --- | --- | --- | --- |
| Laundry Detergent | White | Glows bluish | no | Fluoresce |
| Zinc Sulphide | yellow | Glows yellow | yes | Phosphoresce |
| White paper label | white | Glows with a bluish tinge | no | Fluoresce |
| Neon Paint | Dull color | Glows brightly, same color | no | Fluoresce |
| Glow in the Dark Paint | Dull color | Glows brightly, same color | yes | Phosphoresce |
| Colored Beads | Colored | Glows brightly, same color | yes | Phosphoresce |
| Highlighter on paper towel | yellow | Bright yellow | no | Fluoresce |

III. What kind of light is needed to produce Fluorescence and Phosphorescence?

What do you observe on the vinyl rectangle when you touch it with the

Blue light

White light

Red light

The blue and white light make the material glow.

What kind of light energy is needed to make the vinyl rectangle phosphoresce?	High energy

Observation Sheet

What materials Fluoresce or Phosphoresce?

| Material | What Color is it in room light? | How does it change under the blacklight? | Does it glow after the box lid is closed? | Does it Fluoresce or Phosphoresce? |
| --- | --- | --- | --- | --- |
| Laundry Detergent |  |  | yes no | Fluoresce Phosphoresce |
| Zinc Sulfide |  |  | yes no | Fluoresce Phosphoresce |
| White paper label |  |  | yes no | Fluoresce Phosphoresce |
| Neon Paint |  |  | yes no | Fluoresce Phosphoresce |
| Glow in the Dark Paint |  |  | yes no | Fluoresce Phosphoresce |
| Highlighter on paper towel |  |  | yes no | Fluoresce Phosphoresce |

III. What kind of light is needed to produce Fluorescence and Phosphorescence?

What do you observe on the vinyl rectangle when you touch it with the

Blue light     ________________________________

White light   ________________________________

Red light      ________________________________

What kind of light energy is needed to make the vinyl rectangle phosphoresce?		____

# Text boxes

Visible Light

Is the light hot or cold?

yes

Incandescence

“hot light”

no

Luminescence

“cold light”

Phosphorescence

- continues glowing after

light is removed

Fluorescence

- stops glowing after light

is removed